## Slide 1: BAMBOO STRUCTURES FOR SUSTAINABLE INFRASTRUCTURE
Presented By:
Dr. Chaaruchandra Korde,
Assistant Professor,
Centre for Technology Alternatives for Rural Areas (CTARA),
Indian Institute of Technology, Bombay (IITB)
Technical Director, Greenbam Infratech Pvt. Ltd. (www.greenbam.in)

## Slide 2: Sustainable Infrastructure: Materials, Structures, Technology Development, Demonstration and Dissemination
BAMBOO CONSTRUCTION FOR

## Slide 4: Bamboo Structures

## Slide 5: BACKGROUND
Bamboo Farming
Structural elements (Beam/column/wall)
Bamboo Construction
Background:
Proposal:
106 hector of waste land of Allahabad, India due to brick mining upto 3-4 m depth
UTTHAN with help from INBAR converted it into fertile lands with Bamboo Cultivation
Won US $ 1 million ALCAN Award
Challenges:
Farmers have now fertile lands and are having rapid bamboo growth
Unable to find markets for sale of bamboo
The present markets like paper pulp, fire wood, handicraft, charcoal, etc have lesser consumptions and are giving low returns
(Rapid Growth)
(Rapid Consumption)
--: GAP :--

## Slide 6
HOW TO ACHIEVE A BETTER MOMENT OF INERTIA WITH BAMBOO
STRUCTURAL LOAD BEARING

## Slide 7: BAMBOO To HIB TECHNOLOGY
INDIAN INNOVATION,
FIRST OF ITS KIND IN THE WORLD

## Slide 8: Dendrocalamus strictus
45 % of Indian Bamboo

## Slide 9: TEST SETUPS FOR TESTING ARCHES

## Slide 10: TEST SETUPS FOR TESTING ARCHES

## Slide 11: TEST SETUPS FOR TESTING ARCHES
UNIFORM DISTRIBUTED LOADING SYSTEM FOR ARCH
Proving Ring
Hydraulic Jack
Dial Gauge

## Slide 12: BAMCRETE ARCHES – 4 - 6 M

## Slide 13
OBSERVATIONS
A continuous shift of deformation under cyclic loading for arch B and C
Linear non-elastic flexibility in bamboo (OBATAYA E. ET. AL., 2007)
A progressive increase in the stiffness of the arches with increasing cycles

## Slide 14
Twin Bamboo column with HIB Joint
COLUMN FAILURE/ ULTIMATE LOAD
FAILED BAMBOO COLUMN
FAILURE LOAD: 4500 kg
Korde Chaaruchandra, Ashok Gupta and P. Sudhakar, “Haritha-IITD Bamcrete Technology: A new perspective for Ferro-Bamboo-Concrete Composite Structures”, Indian Journal of Ferrocement, pg. 257, 2011. www.ferrocementindia.com

## Slide 15
TECHNOLOGY DEMONSTRATION
Korde Chaaruchandra, Ashok Gupta and P. Sudhakar, “Haritha-IITD Bamcrete Technology: A new perspective for Ferro-Bamboo-Concrete Composite Structures”, Indian Journal of Ferrocement, pg. 257, 2011. www.ferrocementindia.com
IIT DELHI, 2009
10 YEARS OLD

## Slide 16: MATERIAL TESTING & EQUIP. DEVELOPMENT
(mm)
4000 Kg Load
L/d Ratio = 2
MTS TESTING MACHINE
COST: ~ 100 LACS
LOW COST TEST EQUIPMENT
COMPRESSION TESTING
CYCLIC/FATIGUE TESTING
TENSION TESTS
BENDING TEST
COST: 7-10 LACS….!!

## Slide 17
LOW COST EQUIPMENT DEVELOPED IN HOUSE
ARCH TEST
COMP. TEST
FATIGUE TEST
FATIGUE TEST
CREEP TEST
TENSION TEST
COLUMN TEST
REACTION FRAME
CYCLIC TEST
BENDING TEST

## Slide 18
MULTI-LEVEL BAMBOO STRUCTURE

## Slide 19
MULTI-LEVEL BAMBOO STRUCTURE
OPEN TERRAIN ON 3 SIDES
WIND SPEEDS 150 TO 170 KM/HR
NARROW SPACE & 12 PERSONS TO ACCOMMODATE

## Slide 20
ARCHITECTURAL & STRUCTURAL MODELS

## Slide 21
FEM MODELING

## Slide 22
STRUCTURAL ANALYSIS: 1.5 (D.L + L.L)
Max Deflection = 2.4 mm

## Slide 23
MULTI-LEVEL BAMBOO STRUCTURE

## Slide 24
MULTI-LEVEL BAMBOO STRUCTURE

## Slide 25
MULTI-LEVEL BAMBOO STRUCTURE

## Slide 26
MULTI-LEVEL BAMBOO STRUCTURE

## Slide 27
MULTI-LEVEL BAMBOO STRUCTURE, INDIA

## Slide 28
MULTI-LEVEL BAMBOO STRUCTURE

## Slide 29
MULTI-LEVEL BAMBOO STRUCTURE

## Slide 30
MULTI-LEVEL BAMBOO STRUCTURE

## Slide 31
Multi-level Bamboo Police Barrack
(Madhyanchal Bhawan, New Delhi)
ACKNOWLEDGEMENTS:
Funding agency: M.P. State Bamboo Mission, Gov. of Madhya Pradesh (Dr. Ajoy Bhattacharya & Shri B.B. Singh)
Designed & Built by: Green Bam Infra Tech Pvt Ltd., New Delhi, www.greenbam.in (Start-Up under Start-up India Program)

## Slide 32
Bamboo Senior Citizen Shelter
(Madhyanchal Bhawan, New Delhi)
ACKNOWLEDGEMENTS:
Funding agency: Delhi Development Authority, New Delhi
Designed & Built by: Green Bam Infra Tech Pvt Ltd., New Delhi, www.greenbam.in (Start-Up under Start-up India Program)

## Slide 33
Bamboo Gaushala (Cow Shed)
(at Karma Lakelands, Gurgaon, Haryana)
ACKNOWLEDGEMENTS:
Funding agency: Karma Lakelands, Gurgaon, Haryana
Designed & Built by: Green Bam Infra Tech Pvt Ltd., New Delhi, www.greenbam.in (Start-Up under Start-up India Program)

## Slide 34
Bamboo Yoga Hall
(Delhi Development Authority, New Delhi)
ACKNOWLEDGEMENTS:
Funding agency: Delhi Development Authority, New Delhi
Designed & Built by: Green Bam Infra Tech Pvt Ltd., New Delhi, www.greenbam.in (Start-Up under Start-up India Program)

## Slide 35
ACKNOWLEDGEMENTS:
Funding agency: Karma Lakelands, Gurgaon, Haryana
Designed & Built by: Green Bam Infra Tech Pvt Ltd., New Delhi, www.greenbam.in (Start-Up under Start-up India Program)
Golf Cart Parking Shed
(at Karma Lakelands, Gurgaon, Haryana)

## Slide 43
CHOICE IS OURS
Sustainable Technology
Technology to Just sustain
Artisan Training at IIT Delhi, 2007
2 Bamboo Arch with 3 Nos. of 2 inch diameter Bamboo each, supporting 19 people
JAI HIND